Title Goes Here With Each Initial Letter Capitalized

Author's Name1, Author's Name2, *

1Replace this text with authors' affiliations (use complete addresses)

2If more than one affiliation is needed, they should be indicated by superscripts

The abstract must be in ONE page, single-line spacing and the font used must be Time New Roman 12 point.

Keywords: enter three keywords here.

* Corresponding author’s email: abc@uni.wxy.com

###An abstract template can be found in the next page.

Cytotoxicity and Degradation Behaviour of Potassium Sodium Niobate

Sea-Fue Wang1, Wei-Hsing Tuan2,*

1Institute of Materials Science and Engineering, National Taipei University of Technology, Taipei, Taiwan 106

2Department of Materials Science and Engineering, National Taiwan University, Taipei, Taiwan 106

In the present study, two lead-free piezoelectric ceramics, potassium sodium niobate (K0.5Na0.5NbO3, KNN) and lithium-doped potassium sodium niobate (Li0.06K0.47Na0.47NbO3, LKNN), were prepared by a solid-state reaction process. The cytotoxicity evaluation indicated that the cytotoxicity of KNN is low. However, a strength decrease was noted after soaking in saline solution for 7 days. The addition of 6 mol% Li into the KNN improves its density; the strength and piezoelectric coefficient are enhanced consequently. Nevertheless, the cytotoxicity of LKNN is slightly higher than that of KNN. The higher cytotoxicity is related to the release of Li ions. The release of Li ion also induces the degradation of piezoelectric performance.

Keywords: ferroelectric; abstract; template

* Corresponding author’s email: tuan@ntu.edu.tw